FAQ’s – Welding

1).  What is the difference between shielded metal arc, gas metal arc, fluxed cored arc and submerged arc welding?  (Definitions according to AP-42)

Shielded Metal Arc Welding (SMAW) -

SMAW uses heat produced by an electric arc to melt a covered electrode and the welding joint at the base metal. During operation, the rod core both conducts electric current to produce the arc and provides filler metal for the joint. The core of the covered electrode consists of either a solid metal rod of drawn or cast material or a solid metal rod fabricated by encasing metal powders in a metallic sheath. The electrode covering provides stability to the arc and protects the molten metal by creating shielding gases by vaporization of the cover.

Gas Metal Arc Welding (GMAW) -

GMAW is a consumable electrode welding process that produces an arc between the pool of weld gas and a continuously supplied filler metal. An externally supplied gas is used to shield the arc.

Flux Cored Arc Welding (FCAW) -

FCAW is a consumable electrode welding process that uses the heat generated by an arc between the continuous filler metal electrode and the weld pool to bond the metals. Shielding gas is provided from flux contained in the tubular electrode. This flux cored electrode consists of a metal sheath surrounding a core of various powdered materials. During the welding process, the electrode core material produces a slag cover on the face of the weld bead. The welding pool can be protected from the atmosphere either by self-shielded vaporization of the flux core or with a separately supplied shielding.

Submerged Arc Welding (SAW) -

SAW produces an arc between a bare metal electrode and the work contained in a blanket of granular fusible flux. The flux submerges the arc and welding pool. The electrode generally serves as the filler material. The quality of the weld depends on the handling and care of the flux. The SAW process is limited to the downward and horizontal positions, but it has an extremely low fume formation rate.

2). What SCC Number should I use?

If you use one type of welding wire/rod use the appropriate SCC # as listed below:

| FCAW - E110 | 30905306 |
| --- | --- |
| FCAW - E11018 | 30905308 |
| FCAW - E308LT | 30905312 |
| FCAW - E316LT | 30905320 |
| FCAW - E70T | 30905354 |
| FCAW - E71T | 30905355 |
| GMAW - E308L | 30905212 |
| GMAW - E70S | 30905254 |
| GMAW - ER1260 | 30905210 |
| GMAW - ER316 | 30905220 |
| GMAW - ER5154 | 30905226 |
| GMAW - ERNiCrMo | 30905276 |
| GMAW - ERNiCu | 30905280 |
| SAW - EM12K | 30905410 |
| SMAW - 14Mn-4Cr | 30905104 |
| SMAW - E11018 | 30905108 |
| SMAW - E308 | 30905112 |
| SMAW - E310 | 30905116 |
| SMAW - E316 | 30905120 |
| SMAW - E410 | 30905124 |
| SMAW - E6010 | 30905128 |
| SMAW - E6011 | 30905132 |
| SMAW - E6012 | 30905136 |
| SMAW - E6013 | 30905140 |
| SMAW - E7018 | 30905144 |
| SMAW - E7024 | 30905148 |
| SMAW - E7028 | 30905152 |
| SMAW - E8018 | 30905156 |
| SMAW - E9015 | 30905160 |
| SMAW - E9018 | 30905164 |
| SMAW - ECoCr | 30905168 |
| SMAW - ENi-Cl | 30905172 |
| SMAW - ENiCrMo | 30905176 |
| SMAW - ENi-Cu | 30905180 |

If you use more than one type of wire/rod but all within the same subcategory (shielded metal arc, gas metal arc, fluxed cored arc or submerged arc welding) use the appropriate SCC number listed below:

| Fluxed Cored Arc Welding | 30905300 |
| --- | --- |
| Gas Metal Arc Welding | 30905200 |
| Submerged Arc Welding | 30905400 |
| Shielded Metal Arc Welding | 30905100 |

If you use more than one type of welding wire/rod from multiple subcategories (shielded metal arc, gas metal arc, fluxed cored arc or submerged arc welding) use the following SCC number:  30900501 Arc Welding: General.